## Slide 1: Additively Manufactured High Temperature Friction Stir Tooling through Thermal Spray Techniques
Fardad Azarmi1, Martin McDonnell2
Department of Mechanical Engineering, North Dakota State University, Fargo, ND, 58108, USA.
US ARMY FCDD-GVS.

## Slide 2: Outline
Introduction to Friction Stir Welding (FSW)
FSW Tooling
Introduction to Thermal Spraying
New Design for FSW Tooling System
Project Plan

## Slide 3: Friction Stir Welding (FSW)
The technology was introduced to the industry in 1991 by UK Welding Institute.
A Solid State process capable of producing very high strength joining of a wide range of materials (metals & alloys)
Introduction to FSW
FSW Tooling
Introduction to Thermal Spraying
New Design for FSW Tools
Project Plan

## Slide 4: Friction Stir Welding (FSW)
Advantages
Introduction to FSW
FSW Tooling
Introduction to Thermal Spraying
New Design for FSW Tools
Project Plan
Compared to the Traditional Joining Techniques
Rotational and translational movement of a cylindrical tool on the surface of rigidly clamped parts.
Friction and deformation resulting from tool movement cause plasticization.
Joining of two parts by deformation.
Lower apparent energy input
      Lower cost
      Less distortion
      Less residual stress (build up)
      Process take place entirely in solid state condition
            No melting
            No re-solidification
            Small heat affected zone
            High quality Welding
                No porosity (very low)
                No oxidation (very low)
Application:
            Marine, boats, and ships
            Aerospace
            Military
            Railways
                Automotive
                Electronics
                And more….

## Slide 5: FSW Tooling
Introduction to FSW
FSW Tooling
Introduction to Thermal Spraying
New Design for FSW Tools
Project Plan
Tool Geometry & Materials
Picture Source: https://www.phase-trans.msm.cam.ac.uk/2011/tools.html
Optimum tool design results in high quality welding with desired speed.
Welding efficiency can be highly affected by FSW Tools. Since, the shape and material of the tool play an important role in the heat generation and heat loss during the process.
FSW Tools provide both rotational and weld movement and speed. Force (pressure) is also transferred through tool components on the work piece.
                H13 Tool Steel
                Nickel Cobalt Alloy
                Tungsten Carbide
                Boron Nitride
                ….
FSW Tool Materials:

## Slide 6: FSW Tooling
Introduction to FSW
FSW Tooling
Introduction to Thermal Spraying
New Design for FSW Tools
Project Plan
Low heat generation. (Tools with relatively low COF)
High rate of heat flow to the tool during the process. (damage in Tool and short service life)
Provide inadequate rotation and translation speed.
Breakage of pin (nib) inside the work piece during process. (Low strength Tools and low heat generation)
Restriction in applied pressure on the work piece. (Low strength Tools)
Inability in joining dissimilar materials.
Problems with FSW Tools:
Picture Source: Oak Ridge National Laboratory (ORNL)

## Slide 7: FSW Tooling
Introduction to FSW
FSW Tooling
Introduction to Thermal Spraying
New Design for FSW Tools
Project Plan
High heat generation on the work piece.
Low heat flow to the tool.
Optimize material flow around the nib (pin).
Reduction of heat loss.
Increase of both welding speed and rotation speed.
Increase plasticization of work piece.
Increase tool life.
Lower the cost of the system.
An Optimum Tool Design Will Provide:

## Slide 8
Introduction to FSW
FSW Tooling
Introduction to Thermal Spraying
New Design for FSW Tools
Project Plan
Thermal Spraying
Deposition of a coating layer on the surface of the materials
Increases: base material's resistance to corrosion, erosion,
cavitations, friction, and abrasion.
Fabrication of near net shape parts and components
Fabrication of graded materials (Functionally gradient materials, FGM)

## Slide 9
Introduction to FSW
FSW Tooling
Introduction to Thermal Spraying
New Design for FSW Tools
Project Plan
Thermal Spraying
Powder
Droplet
Splat
Coating
Coating Formation and Build-up Process
Coating Cross-section

## Slide 10
Thermal Spraying Technologies
Combustion
Electric
Kinetic
Low Velocity
High Velocity
Flame spray
HVOF
HVAF
D-Gun TM
Wire arc spray
Plasma
Cold spray
Direct current (DC)
Radio frequency (RF)
Atmospheric
Inert
Shroud
Vacuum
Introduction to FSW
FSW Tooling
Introduction to Thermal Spraying
New Design for FSW Tools
Project Plan
Thermal Spraying

## Slide 11: Hard Coating Research Lab (HCRL) – ME Department (NDSU)
Introduction to FSW
FSW Tooling
Introduction to Thermal Spraying
New Design for FSW Tools
Project Plan
Thermal Spraying
Established in 2013- Funded by EPSCoR IIP Major Equipment
Director: Fardad Azarmi
Automatic Spraying

## Slide 12: Objectives:
Introduction to FSW
FSW Tooling
Introduction to Thermal Spraying
New Design for FSW Tools
Project Plan
New Design For FSW Tools
Develop new tools to advance FSW technology to increase its efficiency and service life, followed by decreasing the maintenance tooling costs.
- We have proposed:
Evaluation of the capability of thermal spray solution for depositing of high temperature materials onto FSW tools.
Utilization of a rapid and affordable technology for deposition of high temperature (refractory) materials.
Apply a hard coating on the surface of FSW tools to improve the performance, increase life, and enhance their appearance.
Develop a near-net shape forming processes by thermal spraying to produce a multifunctional component.
To this end:

## Slide 13: Scope of the Work:
Introduction to FSW
FSW Tooling
Introduction to Thermal Spraying
New Design for FSW Tools
Project Plan
Project Plan
The study will be accomplished in three major categories:
Process Development
B. Property Characterization
C. Post-deposition Development

## Slide 14: Scope of the Work (Continued):
Project Plan
The study will be accomplished in three major categories:
C. Post-deposition Development
Identify an effective heat treatment process to improve properties of the new tools. (Post-deposition process).
Develop a risk management model to quantitatively measure the service life of the new FSW tools. (Risk management)
Evaluate the performance of newly developed FSW tool. (Performance evaluation)
Introduction to FSW
FSW Tooling
Introduction to Thermal Spraying
New Design for FSW Tools
Project Plan

## Slide 15
Acknowledgement
U.S. Army CCDC Ground Vehicle Systems Center

## Slide 16: Questions?